## Slide 1: Material properties

## Slide 2: Fluence of neutrons
F = N/ S = N / pr2
neutrons pass through the imaginary sphere in all directions

## Slide 3
Expression of neutron dose and fluence
The dose coming from neutrons is often expressed in relation to the materials used in the active zone by a quantity known as dpa - displacements per atom - the number of displacements per atom. This quantity is then related to the total fluence.
Typical values for BWR are:
1.5x1021 n/cm2 per 1 dpa for neutron energies E>0.1MeV
0.7x1021 n/cm2 per 1 dpa for neutron energies E>1.0MeV
For PWR (French) it states:
dpa =6.10-22 x fluence for E>0.1MeV
which corresponds
1.67x1021 n/cm2 at 1 dpa for neutron energies E>0.1MeV

## Slide 4: Isotropic volume expansion (swelling)

## Slide 5: Neutron spectra of reactor WWER 440
Boundary of active zone
Outer surface of active zone vessel
Inner surface of reactor pressure vessel
Outer surface of reactor pressure vessel

## Slide 6
 | VVER 440/230 | VVER 440/213 | VVER 1000
Project lifetime | 30 | 40 | 40
 | Maximum fluence (n/cm2) (>0,5 MeV) |  | 
Base material | 2,3 .1020 | 2,6 .1020 | 6,3 .1019
Welding metal | 1,6 .1020 | 1,8 .1020 | 5,7 .1019
 | Maximum fluence (n/cm2) (>1 MeV) |  | 
Base material | 1,4 .1020 | 1,6 .1020 | 3,7 .1019
Welding metal | 1,0 .1020 | 1,1 .1020 | 3,4 .1019

## Slide 9
Hellan Kare: Introdution to Fracture mechanics, McGraw-Hill Book Company, 1984

## Slide 11
Fracture properties of reactor steel (temperature dependence)

## Slide 12
Surveillance Programme